TOWN OF HOLLISTON

REGULATIONS FOR DRIVEWAY OPENINGS

TOWN OF HOLLISTON

HIGHWAY DEPARTMENT

63 ARCH STREET

HOLLISTON, MA  01746

508-429-0615

www.townofholliston.us

TABLE OF CONTENTS

SECTION									PAGE

Definitions									1

Permit Procedures								1

Performance Bonds								1-2

Exemptions									2

Fines and Penalties								2

Special Requirements								3

Emergency Actions								3

Moratorium									3

Restoration of Streets/Driveways						3-4

Temporary Patches								4

Driveway Specifications							5

Driveway Section								6

Scenic Roads									7-8

Notification Schedule								9

New Pavements and Guidelines						10-11

Application Form								12

DEFINITIONS

- “Street” shall mean any accepted street (Public Way) under the jurisdiction of the Town of Holliston.

- “Excavation” shall include the removal of any portion of the existing street, including pavement, curbing, sidewalks, or grass areas.

- “Permit” shall be the written permission for the administering agency, the Highway Department, as appointed by the Board of Selectmen.

PERMIT PROCEDURES

- No person or organization shall make any excavation, including driveway openings or curb cuts, in any street without first obtaining a permit, except as otherwise provided by these regulations.  Permits can be obtained from the Highway Department, Monday through Friday, between the hours of 8:30 a.m. and 3:30 p.m.  Permits must be obtained at least 48 hours before beginning the work.

- At the time of application, $.50 per linear foot with a minimum fee of $50.00 must be paid to cover the costs of inspection services that will be conducted by the Town.  The fee will cover excavation in one location.

- Permits will be issued for a period of one year.  All excavations shall be initiated within six months and permanent repairs shall be completed in full and approved by the Highway Department within one year.  The applicant or his agent shall be fully responsible for all necessary repairs prior to final acceptance.  A performance bond is required, and explained in the following section.

- For Scenic Road requirements, see pages 7 and 8.

PERFORMANCE BOND

- At the time of application for a street opening permit, the applicant shall submit to the Town a performance bond to assure that permanent repairs are properly completed.

- The form of bond shall be either a personal or certified check, payable to the Town of Holliston, or a bond of a surety company authorized to do business in the Commonwealth of Massachusetts.  It shall be conditioned that the applicant shall guarantee the satisfactory performance of the work in all respects, and shall replace or restore any portion of the street in which the applicant or his agent performs excavations.

- The bond shall allow the Town of Holliston to perform work deemed necessary by the Highway Superintendent or his representative to correct any deficiencies, and all costs incurred by the Town to complete the repair or correct deficiencies may be applied against the bond.

- Upon satisfactory completion of permanent repairs, final acceptance in writing by the Highway Department, the balance of the bond will be returned in full to the applicant.

- The amount of the bond shall be calculated at a rate of $90.00 per square yard or area disturbed at driveway installations.  It shall be assumed that the disturbed area will extend four feet beyond each edge of the proposed final driveway apron.

EXEMPTIONS FROM PERMITS AND BONDS

- The Town of Holliston departments will not be required to pay a fee or post a bond, but they will be required to obtain a permit.

- No permit or bond will be required for incidental grading and landscaping work performed by property owners on unpaved frontage areas within the public right of way.  This clause shall in no way diminish the Town authority over said areas.

- Bonds from public utility companies that are self-insured will be acceptable if the terms and conditions are similar to those outlined herein.

- Public utility companies may be allowed to pay fees on an annual or periodic basis at the discretion of the Board of Selectmen.

FINES AND PENALTIES

Failure to obtain a permit as required in these regulations before commencing work or, having obtained a permit, failure to comply with these regulations, shall be subject to a fine not to exceed $100.00 for each offense, pursuant to the Town Bylaws.  Each day in which violation continues shall constitute a separate offense.  For purposes of these regulations, the Highway Superintendent shall be the enforcement officer.

No further work will be allowed by the contractor in the Town of Holliston until all alleged improprieties have been resolved to the satisfaction of the Highway Superintendent.

Any person accused of violating these rules or regulations shall be notified of the alleged violation, in writing, via certified mail, return receipt requested, which shall set forth a date and time at which a hearing will be held before the Highway Superintendent or his designee in order to afford the person an opportunity to be heard in regard to the alleged violation, with or without counsel, as the person shall choose.

SPECIAL REQUIREMENTS

- No public way shall be opened prior to April 15th or after November 15th.

- No public way shall be blocked overnight, and daytime blockage shall be kept to a minimum.  If police traffic control is required, costs shall be paid by the applicant, in addition to the fees specified herein.

- The applicant or his agent shall be fully responsible for the work, including traffic control and public safety, at all times.

- All repairs shall be completed in full, and approved within the specified duration.

- Not excavations shall remain open overnight.

EMERGENCY ACTIONS

- Nothing in these regulations shall prevent the making of such exaction as may be necessary for the preservation of life or property, or for the location of trouble, or repairing conduit, cable or pipe.

- A permit shall be applied for the first working day after emergency work is commenced.

MORATORIUM

- No permits will be issued for the excavation of paved surfaces on streets that have been reconstructed, or resurfaced, or are newly constructed and accepted by the Town, within five years following the installation of new street surfaces, except in the case of extreme emergency or hardship, as approved by the Board of Selectmen.

- Special permits, on an individual case basis, may be issued for extreme emergency or hardship as approved by the Board of Selectmen.  Jacking or tunneling without disturbing the road pavement may be required.  “After the Fact” restoration resulting from extreme emergency work will be performed to standards established for each case to assure that the patch will have a life expectancy equal to surrounding pavement.

BACKFILL AND RESTORATION – STREETS AND DRIVEWAYS

- The intent of these regulations is to assure that the street is restored to a condition at least equal to its condition prior to excavation.

- Trench backfill material may be approved material from the excavations, or granular borrow material.  Frozen or saturated material shall not be used.

- Backfill shall be compacted by mechanical compactors, in twelve inch layers, to 90% of optimum dry density.

- In paved areas constructed during or after 1987 the pavement restoration, including gravel base courses, shall conform to the typical sections and requirements of the current Planning Board Rules and Regulations for new streets.

- Adjoining edges of existing pavement shall be trimmed to a vertical face and coated with rubberized asphalt crack sealer before placing the bituminous pavement patch.

- Any roadway appurtenances, such as signs, curbs, pavement markings, etc. that are disturbed by the work shall be restored to their original locations.

- Construction details not specified herein shall conform to details furnished by the Highway Department at the time of application.

TEMPORARY PATCHES

- Temporary pavement patches may be made for emergency work, winter work, or where permanent paving is not feasible immediately following backfill as determined by the Highway Superintendent or his representative.

- The temporary pavement may be bituminous “cold patch” material, and is to be a minimum of four inches compacted thickness.

- Temporary patches shall be maintained by the permit holder.  Any holes or depressions which may occur shall be filled so as to keep the surface in a safe condition for traffic.

- Temporary patches shall be removed and replaced with permanent patches as soon as possible, and whenever directed by the Highway Superintendent or his representative.

DRIVEWAY SPECIFICATIONS

Residential/Commercial:

- The location of each driveway opening shall be approved in writing by the Highway Department before any work is started.

- Driveways shall be constructed in accordance with the attached detail and listed dimensions:

A. Residential Drives:  Width minimum 8’		Maximum 16’

Radius minimum 5’		Maximum 10’

B. Commercial Drives:  Width minimum 20’	Maximum 24’

Radius minimum 20’	Maximum 30’

- Where driveway construction crosses existing drainage courses at the edge or adjacent to the edge of the traveled way of any street, a culvert shall be installed to maintain free flow of run-off.  The size and method of placement shall be as directed by the highway Superintendent or his representative.

- The area between the edge of the street pavement and the right of way line or minimum of ten feet shall be excavated of all clay and subsoil, other than gravel.  Such excavation shall be back-filled with good quality bank gravel or dense graded crushed stone and thoroughly compacted in twelve inch layers to a 90% dry density below finish grade with a mechanical compactor.

- Over the gravel base shall be constructed a bituminous concrete pavement.  It shall be placed in two courses:

  - Residential: Two inch bituminous concrete base and one inch bituminous concrete top, having a total thickness of three inches after compaction with a self-propelled roller having a minimum weight of five tons.

  - Commercial: Two and a half inches bituminous base and one and a half inch bituminous concrete top, having a total thickness of four inches after compaction with a self-propelled roller having a minimum weight of five tons.

Upon completion of construction of the driveways, the Highway Department shall be notified.

(Street Name)_________________________________________is a new (residential or industrial) road surface within the last five years, and is on the restricted list for openings.  This permit is issued under the hardship provision in our Street Regulations for Excavations and, in addition to the requirements for restoration, infrared treatment at the time of the permanent patch must be performed to blend the patch with the new road surface.

GUIDELINES FOR:

____________________________________________________________________________

(Street Name)

- Compact trench every foot.

- Last foot to be gravel base processed material.

- If Residential: Minimum two and a half inched of binder and one and a half inches of top or to match existing, if that sum is greater.

- If Industrial: Minimum three and a half inches of binder and one and a half inches of top or to match existing, if that sum is greater.

- Infrared treatment is required to blend patch with new road surface, as noted above.

15c. DESIGNATION OF SCENIC ROADS:		MAINTENANCE, ETC.

Upon recommendation or request of the Planning Board, Conservation Commission, or Historical Commission of any City or Town, such City or Town may designate any road in said City or Town, other than a numbered route or State Highway, as a scenic road.

After a road has been designated as a scenic road, any repair, maintenance, reconstruction, or paving work done with respect thereto shall not involve or include the cutting or removal of trees, or the tearing down or destruction of stone walls, or portions thereof, except with the prior written consent of the Planning Board, or if there is no Planning Board, the Selectmen of a Town, or the City Council of a City, after a public hearing duly advertised twice in a newspaper of general circulation in the area, as to the time, date, place and purpose, the last publication to occur at least seven days prior to such hearing; provided, however, that when a public hearing must be held under the provision of this section and under section three of chapter eighty-seven prior to the cutting or removal of a tree, such hearings shall be consolidated into a single public hearing before the Tree Warden and Planning Board, or if there is no Planning Board, the Selectmen of a Town, or the City Council of a City, and notice of such consolidated public hearing shall be given by the Tree Warden or his deputy as provided in said section three of chapter eighty-seven.*

Designation of a road as a scenic road shall not affect the eligibility of a City or Town to receive construction or reconstruction aid for such road pursuant to the provision of chapter ninety.  (1973, 67: 1979, 552)

Editorial Note:

The 1979 amendment affected the second paragraph, adding a provision for consolidated hearings where public shade trees are involved.

*	In the event that trees or stone walls will not be cut or disturbed, the applicant shall submit a notarized letter stating the project will not involve cutting or removing trees nor tearing down or disturbing stone walls, or portions thereof.

TOWN OF HOLLISTON

SCENIC ROADS

Designated & Approved – May 15, 1975 – (Article 15)

Adams Street

Bullard Street

Courtland Street

Hanlon Road

Hill Street

Jennings Road

Marshall Street

Prentice Street

Designated & Approved – May 13, 1976 – (Article 26)

Bullard Lane

Central Street

Fisher Street

Fiske Street

Gorwin Drive

Granite Street

Highland Street

Linden Street

Mellen Street

Mill Street

Norfolk Street

Rockland Street

Underwood Street

Wilson Road

Winter Street

Designated & Approved – May 8, 1991 – (Article 27)

Brook Street

High Street

Locust Street

Oak Street

NOTIFICATION SCHEDULE

In the event a Town roadway is to be partially or completely closed to traffic for any period of time, please complete the following procedure:

Permission to close must be received from the Police Department:  508-429-0612.

Notify the Fire Department:  508-429-4631.

During weekdays – School Department Bus Coordinators:

School Dispatch – 508-429-0654

Holmes Transportation – 508-528-4550

Should blasting work be needed, permit must be obtained from the Fire Department.

After notifying the above departments, an Applicant must notify the Highway Department of compliance to Notification Schedule of partial or complete closure.